## Slide 1: Reconstruction of momentum density and determination of one-electron reduced density matrix
Zeyin YAN
Membres du Jury: |  | 
Rapporteur | Dr. Carlo Gatti | University of Milan
Rapporteur | Pr. Enrique Espinosa | Université de Lorraine
Examinateur | Pr. Claude Lecomte | Université de Lorraine
Examinateur | Pr. Nour-Eddine Ghermani | Université Paris-Sud
Examinatrice | Dr. Béatrice Gillon | CNRS, LLB (CEA -Saclay)
Examinateur | Dr. Alessandro Erba | University of Torino
Directeur de thèse | Pr. Jean-Michel Gillet | CentraleSupélec
NNT : 2018SACLC001

## Slide 2: Overview
Introduction
1. Electron densities in position and momentum spaces
  Position space representations
  Momentum space representations
  ‘‘Super-position’’ construction
2. Periodic 1-RDM by a cluster construction
  Cluster construction
  Phase space functions
  Orbital resolved 1-RDM
3. Experimental 1-RDM refinement
  Refinement model
  Results
Conclusions and perspectives
Notes: Short introduction
1, 2, 3
Conclusions…

## Slide 3: Electron density
Electron density is a key for understanding the material properties
Introduction
Ab-initio computations
  Hartree-Fock (HF) : wave-functions
  Density functional theory (DFT) : Kohn-Sham orbitals[1]
  Molecular or periodic computations
charge
position
momentum
spin
[1] Stowasser. R., & Hoffmann. R. (1999).
position
momentum

## Slide 4: Electron density
Experimental observations
Introduction
X ray diffraction
(XRD)
Polarized neutron diffraction
(PND)
Compton scattering
(CS)
Magnetic Compton scattering
(MCS)
Maximum entropy method
(model free)
Independent atoms model
Hansen-Coppens model
…
Techniques
Observations
Electron
densities
Refinement
models
Maximum entropy method
(model free)
Atomic orbital model
Hansen-Coppens model
…
Reconstruction method
(model free)
…
Reconstruction method
(model free)
…
‘spin-split’ model[1,2]
Joint
refinement
[1] Deutsch, M. et al., 2012
[2] Deutsch, M. et al., 2014
[3] Macchi, P. et al., 2015
position space
momentum space
The whole is more than the sum of its parts[3]
Joint models??

## Slide 5: 1-RDM
One-electron Reduced Density Matrix (1-RDM)[1]
Introduction
Connection with position and momentum spaces
[1] Löwdin. P. O. (1955).
Spin-resolved 1-RDM
1-RDM is a natural quantity to connect both position and momentum spaces
Diagonal
Off-diagonal
--
--
position
momentum

## Slide 6: Objectives
Electron density research in position and momentum spaces
Coherence between different experimental data (qualitative)
Experimental 1-RDM refinement (quantitative)
Theoretical 1-RDM computation for periodic case
Introduction
Notes: Qualitative
Quantitative

## Slide 7: Overview
Introduction
Electron densities in position and momentum spaces
  Position space representations
  Momentum space representations
  ‘‘Super-position’’ construction
Periodic 1-RDM by a cluster construction
  Cluster construction
  Phase space functions
  Orbital resolved 1-RDM
Experimental 1-RDM refinement
  Refinement model
  Results
Conclusions and perspectives

## Slide 8: YTiO3 perovskite
2.024 Å
2.025 Å
2.08 Å
O2
O1
O2
’
Ferromagnetic below Tc=29K
  Space group: Pnma
YTiO3
TiO6 octahedra
2.08 Å
2.025 Å
Ti—O2’
O2—Ti
Notes: Most importantly, this crystal is stable for XRD, PND and MCS
O2 and O2’

## Slide 9: 3d-orbital splitting
2.024 Å
2.025 Å
2.08 Å
O2
O1
O2
’
Ti 3d-orbital splitting due to crystal field
YTiO3
Akimitsu. J, et al (2001).
Ti 3d-orbital
E
octahedron field
elongation along z
Notes: Due to the crystal field effect
Confirmed by Akimitsu with PND data

## Slide 10: Ti—O—Ti spin coupling
Spin coupling pathways
YTiO3
Ti—O1—Ti
Ti—O2—Ti
Ti(3d)—O(2p)—Ti(3d) spin coupling
2.024 Å
2.08 Å
2.025 Å
2.024 Å
Respective roles of O1 and O2 need to be clarified
Ti—O2’
O2—Ti
Notes: In O1 case, two Ti atoms on both sides are at the same distances

## Slide 11: Basic knowledge
Periodic computation (CRYSTAL14[1,2])
  DFT PBE0-1/3[3]
  ECP basis set for Y[4] and Ti[5] and standard basis set (8-411d11f) for O[6]
  spin value per Ti atom
Polarized neutron diffraction (PND) (by collaborators at LLB)
  6T2
  5K and 5T
  286 reflections (unique)
Electron density in position space
[1] Dovesi. R, et al (2014).
[2] Dovesi. R, et al, CRYSTAL14 User's Manual (2014).
[3] Guido, C. A. et al (2013).
[4] unpublished data, offered by the CRYSTAL14 site http://www.crystal.unito.it/Basis_Sets/yttrium.html
[5] Piskunov, S. et al (2004).
[6] Erba, A. et al (2013).

## Slide 12: Refinement models
Hansen-Coppens model[1]
Electron density in position space
[1] Hansen & Coppens (1978).
[2] Deutsch et al (2012).
Spherical core
Spherical valence
Deformation valence
‘‘Spin split’’ model[2]

## Slide 13: Refinement models
Maximum entropy method (MEM)[1]
Electron density in position space
[1] Papoular, R. J., & Gillon, B. (1990).
[2] Gillon, B., & Becker, P. (2011).
Atomic orbital model[2]
MEM and atomic orbital model results will be presented
MEM and atomic orbital model refinements are conducted by I. A. Kibalin and collaborators at LLB
Joint refinement results will be presented in the thesis of Voufack, A. B. (PhD student at CRM2)
Notes: Entropy is the sum of entropy up and down

## Slide 14: Results
Atomic orbital model Ti 3d-orbital (PND)
Electron density in position space

## Slide 15: Results
Spin density in O1—Ti—O2’ plane
Electron density in position space
MEM
Atomic orbital model
Periodic ab-initio
O2
O1
O2
’
Notes: Only spherical functions defined for O1 in refinement model

## Slide 16: Results
Spin density by atomic orbital model
Electron density in position space
O1—Ti—O2’
O2—Ti—O2’
O1—Ti—O2
Local axes:
xz
yz
xy
PND:
O2
O1
O2
’

## Slide 17: Overview
Introduction
Electron densities in position and momentum spaces
  Position space representations
  Momentum space representations
  ‘‘Super-position’’ construction
Periodic 1-RDM by a cluster construction
  Cluster construction
  Phase space functions
  Orbital resolved 1-RDM
Experimental 1-RDM refinement
  Refinement model
  Results
Conclusions and perspectives

## Slide 18: Momentum space
Electron density in momentum space
v//
N(v//)
v⏊
N(v⏊)

## Slide 19: Basic knowledge
Theoretical computation
Electron density in momentum space
Magnetic Compton scattering (MCS) (conducted at Spring8)
  BL08W
  2.5T
  10K ~ 18K
  resolution 0.4 a.u.
  12 directions (3 principal axes + 3 in each plane)
(data was treated by M. Brancewicz)
Directional magnetic Compton profiles (DMCPs)
a
c
b

## Slide 20: DMCPs
Electron density in momentum space
Experimental DMCPs
Theoretical DMCPs
Theoretical DMCPs
convoluted with experimental resolution
Gaussian filter is used for convolution
DMCPs in (ac) plane

## Slide 21: Two-dimensional reconstruction
Electron density in momentum space
Since
Two-dimensional reconstruction method[1]
[1] Tanaka, Y., Sakurai, Y, et al (2001).
FFT
Interpolation
IFFT

## Slide 22: 2D-MEMD
Electron density in momentum space
Two-dimensional magnetic electron momentum density (2D-MEMD)
  (ac) plane
Experimental
Theoretical (convoluted)

## Slide 23: Anisotropy
Electron density in momentum space
Experimental
Theoretical (convoluted)
  (ac) plane
Primitive cell:
340 electrons 4 unpaired electrons (less than 2%)

## Slide 24: Error analysis
Electron density in momentum space
Error propagation analysis
Compton Scattering
Generate random from Gaussian distribution
Normalization
Reconstruction
Statistical analysis
Computation N times

## Slide 25: Error analysis
Electron density in momentum space
Propagated error
  (ac) plane with N=1000
Notes: Our 2D reconstruction gives a good quality result

## Slide 26: ‘‘Super-position’’
a
c
b
a
c
b
An qualitative method to connect position and momentum spaces
‘Super-position’ construction
Experimental
Theoretical
’super-position’ spin density
2D-
  (ac) plane
2D-MEMD
Momentum space
3D spin density
Position space
Coherence ?

## Slide 27: ‘‘Super-position’’
Cross-checking between PND and MCS
‘Super-position’ construction
2D-‘‘super-position ’’ spin density
(Position space)
2D-MEMD
(Momentum space)
Geometric similarity between position and momentum results
  (ac) plane
Limitation: a single type of atom is responsible for a major part of spin density
Notes: It works better for the crystal where a single …
For YTiO3 case, the major spin contribution comes from Ti atom

## Slide 28: Isolated Ti model
PND 3d-orbital (atomic orbital model)
Isolated Ti model
Reproduction of 2D-’super-position’ spin density
2D-‘‘super-position’’ spin density:
(ab)
(ac)
(bc)
2D-MEMD:
(ab)
(ac)
(bc)
Ti—O1—Ti is a possible spin coupling pathway
Ti—O1
Ti—O2
Ti and O construction
Isolated Ti Model
MCS construction
Calculation of 2D-MEMD
Notes: So the simplest model we can consider is the one

## Slide 29: Overview
Introduction
Electron densities in position and momentum spaces
  Position space representations
  Momentum space representations
  ‘‘Super-position’’ construction
Periodic 1-RDM by a cluster construction
  Cluster construction
  Phase space functions
  Orbital resolved 1-RDM
Experimental 1-RDM refinement
  Refinement model
  Results
Conclusions and perspectives

## Slide 30: Motivations
Capacity of gathering position and momentum spaces
Periodic 1-RDM
Diagonal -- position
Off-diagonal -- momentum
Computational challenges
  1-RDM
  Phase space functions
  Cross-term analysis

## Slide 31: Cluster construction
Periodic 1-RDM
A cluster of 27 cells (a Rubik’s magic cube) is extracted from the periodic computation
The primitive cell is where we want to calculate the properties
Contributions from all the 26 first neighboring cells around are accounted for
Periodic ab-initio computation
(CRYSTAL 14)

## Slide 32: Validation
Periodic 1-RDM
In position space
CRYSTAL 14
27-cell cluster construction
Difference

## Slide 33: Validation
Periodic 1-RDM
In momentum space
CRYSTAL 14
27-cell cluster construction
Difference
Reproduction both in position and momentum spaces by cluster construction

## Slide 34: 1-RDM
Periodic 1-RDM
Ti—O1—Ti
Ti—O2—Ti
2.024 Å
2.025 Å
2.08 Å
2.024 Å
Difference between O1 and O2 can be clarified by 1-RDM
: cross-term between two atoms

## Slide 35: Cross-term analysis
Regroup the orbitals
Periodic 1-RDM
: atomic orbitals
If A and B are the same atom,
the result is atomic contribution
If A and B are different atoms,
the result is cross-term contribution
Notes: more specifically, TiO1 and TiO2

## Slide 36: Cross-term analysis
In position space:
Periodic 1-RDM
Weakness of cross-term contribution confirms the legitimacy of refinement model in position space

## Slide 37: Cross-term analysis
In momentum space:
Periodic 1-RDM
Ti—O1—Ti
Ti—O2—Ti
Different behaviors for TiO1 and TiO2
Notes: Basin: O1 83.869, O2 84.145

## Slide 38: Cross-term analysis
1-RDM:
Periodic 1-RDM
Ti—O1—Ti
Ti—O2—Ti
2.024 Å
2.025 Å
2.08 Å
2.024 Å
Cross-term is as important as atomic contribution in 1-RDM representation
Cross-term
Cross-term

## Slide 39: Overview
Introduction
Electron densities in position and momentum spaces
  Position space representations
  Momentum space representations
  ‘Super-position’ construction
Periodic 1-RDM by a cluster construction
  Cluster construction
  Phase space functions
  Orbital resolved 1-RDM
Experimental 1-RDM refinement
  Refinement model
  Results
Conclusions and perspectives
Notes: Now that we have an ab-initio 1-RDM, the question that naturally arises is how it compares with an experimental 1-RDM, especially in O1 cross-term regions.
Here are the preliminary results of our attempts to define a refinement strategy

## Slide 40: 1-RDM refinement model
Cluster approach:
Experimental 1-RDM
: point charge at nuclei positions
O
1
O
1
O
1
O
1
S. Gueddida, Z. Yan, J. M. Gillet, Acta Crystallographica Section A: Foundations and Advances. (2017) (accepted)
S. Gueddida, Z. Yan, J. M. Gillet,." Physical Chemistry Chemical Physics. (2018) (submitted)
Notes: As a minimal model to account for O1 coupling, two neighboring Ti and point charges

## Slide 41: 1-RDM refinement model
Basis set optimization (only radial functions):
Experimental 1-RDM
Gaussian type orbitals (GTOs):
Hansen-Coppens:
P. Becker & P. Coppens. Acta Cryst. (1985).

## Slide 42: 1-RDM refinement model
Molecular occupation refinement:
Experimental 1-RDM
CASSCF-like method:
CASSCF: Complete active space self-consistent field
Occupied
Unoccupied
Fermi level
Core
Active
Virtual
SCF orbitals
CASSCF orbitals
Active
optimized orbitals
refined orbitals

## Slide 43: 1-RDM refinement model
Process
Experimental 1-RDM
Gas phase
ab-initio calculation
Gas phase
ab-initio calculation
Compute and
Minimization of
Compute and
Minimization of
Convergence
YES
NO
YES
NO
Basis set optimization
Occupation refinement
Energy minimization
Algorithm is implemented by S. Gueddida

## Slide 44: 1-RDM refinement model
O
1
O
1
Application on YTiO3
Experimental 1-RDM
  Gas phase ab-initio calculation is conducted with Gaussian 09, using HF/6-31G
  Point charge values: CRYSTAL 14 TOPOND analysis
  Theoretical and (with CRYSTAL 14) with adding noisy are used as “pseudo experimental observations”
  1-RDM by Cluster construction is used as reference (CRYSTAL 14)
  Only Ti—O1—Ti 1-RDM is compared with reference
Notes: HF/6-31G minimal quantum chemistry model
This periodic computation with Xtal14 uses DFT with extended basis set, this is also to make difference with initio guess

## Slide 45: Results
O
1
O
1
Experimental 1-RDM
Reference
1-RDM
G09
1-RDM
Basis set
1-RDM
Occupation
1-RDM
Gas phase
ab-initio calculation
Gas phase
ab-initio calculation
Compute and
Minimization of
NO
Basis set optimization
YES
Compute and
Minimization of
Convergence
YES
NO
Occupation refinement
Notes: Upper_half triangle

## Slide 46: Overview
Introduction
Electron densities in position and momentum spaces
  Position space representations
  Momentum space representations
  ‘‘Super-position’’ construction
Periodic 1-RDM by a cluster construction
  Cluster construction
  Phase space functions
  Orbital resolved 1-RDM
Experimental 1-RDM refinement
  Refinement model
  Results
Conclusions and perspectives
Notes: To conclude this presentation

## Slide 47: Conclusions and perspectives
Conclusions
  ‘‘Super-position’’ method allows a cross-checking between PND and MCS
  Possible spin coupling pathway Ti—O1—Ti can be estimated by ‘isolated Ti model’
  Periodic 1-RDM can be computed by a cluster construction approach
  More information can be extracted and be clarified from 1-RDM and cross-terms analysis
  Experimental 1-RDM refinement is under progress using PND and MCS data
Experimental 1-RDM
Notes: Let me summarize some key points:

## Slide 48: Conclusions and perspectives
Perspectives
  Probability distribution functions in phase space can be further developed
  Experimental data should be used in experimental 1-RDM refinement
  Debye-Waller factors effects should be implemented in the refinement code
Experimental 1-RDM

## Slide 49: Thanks for your attention!
S. Casassa (CRYSTAL 14)
Collaborators:
  CRM2
    C. Lecomte, M. Souhassou, N. Claiser, A. B. Voufack, I. A. Kibalin, F. Morini
  LLB
    B. Gillon, A. Goukassov, F. Porcher
  Spring8
    Y. Sakurai, M. Brancewicz, M. Itou, M. Ito
  SRSMC
    A. Genoni, M. Marazzi
  SPMS
    P. Cortona, S. Gueddida, P. Becker

## Slide 51: Backup slides

## Slide 52: Results
Spin density in O2—Ti—O2’ plane
Electron density in position space
MEM
Atomic orbital model
Periodic ab-initio
O2
O1
O2
’

## Slide 53: Results
Spin density in O1—Ti—O2 plane
Electron density in position space
MEM
Atomic orbital model
Periodic ab-initio
O2
O1
O2
’

## Slide 54: DMCPs
Electron density in momentum space
Experimental DMCPs
Theoretical DMCPs
convoluted with experimental resolution
Gaussian filter is used for convolution
DMCPs in plane (ab)

## Slide 55: DMCPs
Electron density in momentum space
Experimental DMCPs
Theoretical DMCPs
convoluted with experimental resolution
Gaussian filter is used for convolution
DMCPs in plane (bc)

## Slide 56: 2D-MEMD
Electron density in momentum space
Two-dimensional magnetic electron momentum density (2D-MEMD)
  plane (ab)
Experimental
Theoretical
(convoluted)

## Slide 57: 2D-MEMD
Electron density in momentum space
Two-dimensional magnetic electron momentum density (2D-MEMD)
  plane (bc)
Experimental
Theoretical
(convoluted)

## Slide 58: Anisotropy
Electron density in momentum space
  plane (ab)
Experimental
Theoretical
(convoluted)

## Slide 59: Anisotropy
Electron density in momentum space
  plane (bc)
Experimental
Theoretical
(convoluted)

## Slide 60: Error analysis
Electron density in momentum space
Propagation error
  plane (ab)

## Slide 61: Error analysis
Electron density in momentum space
Propagation error
  plane (bc)

## Slide 62
‘‘Super-position’’

## Slide 63: ‘Super-position’
‘Super-position’ construction
Site 1
Site 2
Site 3
Site 4

## Slide 64: ‘Super-position’
‘Super-position’ construction
Site 1
Site 2
Site 3
Site 4

## Slide 65: ‘Super-position’
‘Super-position’ construction
Site 1
Site 2
Site 3
Site 4

## Slide 66: ‘Super-position’
Cross-checking between PND and MCS
‘Super-position’ construction
2D-’super-position’ spin density
2D-MEMD
  plane (ab)

## Slide 67: ‘Super-position’
Cross-checking between PND and MCS
‘Super-position’ construction
2D-’super-position’ spin density
2D-MEMD
  plane (bc)

## Slide 68: Validation
Periodic 1-RDM

## Slide 69: Moyal
Periodic 1-RDM

## Slide 70: Cross-terms analysis
Regroup the orbitals
Periodic 1-RDM
: atomic orbitals

## Slide 71: Cross-terms analysis
Two centers case with 1 electron
Periodic 1-RDM
occupied
unoccupied
Atomic contribution of A
Atomic contribution of B
Cross-term contribution of AB

## Slide 72: 1-RDM refinement model
Spin density (Ti—O1—Ti):
Experimental 1-RDM

## Slide 73: 1-RDM refinement model
Spin density (O1—Ti—O2’):
Experimental 1-RDM
2.08 Å

## Slide 74: 1-RDM refinement model
Spin density (O1—Ti—O2):
Experimental 1-RDM
2.025 Å

## Slide 75: 1-RDM refinement model
DMCP:
Experimental 1-RDM

## Slide 76: 1-RDM refinement model
DMCP:
Experimental 1-RDM

## Slide 77: 1-RDM refinement model
2D-MEMD (ab):
Experimental 1-RDM

## Slide 78: 1-RDM refinement model
2D-MEMD (ac):
Experimental 1-RDM

## Slide 79: 1-RDM refinement model
2D-MEMD (bc):
Experimental 1-RDM

## Slide 80: HOMO
3 HOMOs
Experimental 1-RDM

## Slide 81: LUMO
3 LUMOs
Experimental 1-RDM

## Slide 82: Structure
Cell parameters
  Space group 14
  a=9.65862, b=19.482 , c=9.34,
  spin value: per molecule
Experimental
  XRD[1] and PND[2] data
  Joint refinement by collaborators at CRM2
Theoretical
  Peoridic computation (CRYSTAL14)
  Molecular computation (Gaussian 09)
  CASSCF (Molcas) by collaborators at SRSMC
Nit(SMe)Ph
[1] Pillet, S. et al (2001)
[2] Pontillon, Y. et al (1999)
[3] Pontillon, Y. et al (1999)

## Slide 83: Electron density
Experimental
Nit(SMe)Ph

## Slide 84: Electron density
Theoretical (Gaussian 09)
Nit(SMe)Ph

## Slide 85: Electron density
Spin population
Nit(SMe)Ph

## Slide 86: Two-dimensional reconstruction
Electron density in momentum space
Since
Two-dimensional reconstruction method[1]
denotes a sum which includes all terms, except that the first and the last term are multiplied by
[1] Tanaka, Y., Sakurai, Y, et al (2001).

## Slide 87: Akimitsu

## Slide 88
a
c
b
a
c
b
a
c
b
a
c
b